SPAR, Inc.		   GENERAL DUTY SPECIALTIES

# REFRACTORY SPECIALISTS				PRODUCT DATA

#### SPARCAST 28

SPARCAST 28  is a high strength, general duty refractory castable.   It can be installed by gunning or casting.

###### PHYSICAL PROPERTIES

## Maximum Service Temperature				2800(F

Dry Castable Requirement					127 - 133 lbs./cu.ft.

Typical Mix Water Required 					1.25 – 1.50 gal./110 lbs.

## Bulk Density (at 230(F)					125-130 lbs./cu.ft

## Modulus of Rupture

After Drying at 230(F					300-600 lbs/sq.in.

After Heating to 1500(F				300-600 lbs/sq.in

After Heating to 2250(F				300-700 lbs/sq.in

## Cold Crushing Strength

After Drying at 230(F					2000-4500 lbs/sq.in.

After Heating to 1500(F				2000-4500 lbs/sq.in

After Heating to 2250(F				2000-6000 lbs/sq.in

## Linear Change, %

After Drying at 230(F					0.0 to -0.4

After Heating to 1500(F				0.0 to -0.5

After Heating to 2250(F			            0.0 to -0.6

## Typical Chemical Analysis, %

Al2O3							48.3

SiO2							42.8

CaO							  5.7

TiO2							  1.9

Fe2O3							  1.0

MgO							  0.1

Alkalies						  0.2

SPARCAST 28 is available in 55# bags and bulk bags, palletized and shrink-wrapped.

NOTE: CASTABLE MUST BE STORED IN DRY PLACE

Data shown are average results of standard ASTM tests unless otherwise noted.  Results may vary subject to variations in manufacturing, testing, and installation procedures in the field.

P.O. Box 909, Jacksonville, AL 36265		Phone: (256) 435-9342		Fax: (256) 435-9373